Specific Heat Capacity Table

| Substance | Specific Heat Capacity at 25oC in J.kg-1.oC-1 |
| --- | --- |
| H2 gas | 14,300 |
| He gas | 5,300 |
| H2O(l) | 4,184 |
| lithium | 3,560 |
| ethyl alcohol | 2,460 |
| ethylene glycol | 2,200 |
| ice @ 0oC | 2,010 |
| steam @ 100oC | 2,010 |
| vegetable oil | 2,000 |
| sodium | 1,230 |
| air | 1,020 |
| magnesium | 1,020 |
| aluminum | 900 |
| Concrete | 880 |
| glass | 840 |
| potassium | 750 |
| sulphur | 730 |
| calcium | 650 |
| iron | 444 |
| nickel | 440 |
| zinc | 390 |
| copper | 385 |
| brass | 380 |
| sand | 290 |
| silver | 240 |
| tin | 210 |
| lead | 160 |
| mercury | 140 |
| gold | 129 |